EMI / RFI  Shielding  Products

ISO  9001:2000  REGISTERED

“MAJR  Difference  MAJR  Satisfaction”

“MAJR  Difference  MAJR  Satisfaction”

PRODUCT

DATA  SHEET

DS-7.2.1-SAL  2-29-12

Conductive Fluorosilicone Elastomer  (5000 Series)

Product Summary

This conductive fluorosilicone elastomer material is a unique composite of high quality fluorosilicone and conductive Silver Nickel (Ag/Ni) microscopic particles.

Product Application

This conductive elastomer is a unique composite of high quality fluorosilicone and conductive microscopic particles, manufactured to strict formulations, yielding a gasketing material that meets military MIL-DTL-83528 (Type L) and commercial electronic requirements.  The fluorosilicone material is a synthetic rubber useful in applications involving petroleum oils, fuels, and silicone oils, with the same operating temperature as silicone.

The surface that this material is to be applied

to must be conductive, meaning no non-conductive paint, oils, or coatings.  If a non-conductive surface is present on the mating or mounting surface the conductive elastomer, shielding effectiveness will be greatly degraded.

Contact MAJR Products Corporation for product configurations and part numbers.

Product Technical Data

| Electrical Specifications | Tolerance | Test Method | Silver Aluminum fluorosilicone Elastomer (Ohm-cm) |
| --- | --- | --- | --- |
| Volume Resistivity | Maximum | MIL-DTL-83528 (PARA 4.6.11) | 0.005 |
| Shielding Effectiveness (Frequencies) | Minimum | MIL-DTL-83528 (PARA 4.5.12) | Silver Aluminum Elastomer (Attenuation - dB) |
| 20 MHz (E-Field) | Minimum | (PARA 4.5.12) | 100 |
| 500 MHz (E-Field) | Minimum | (PARA 4.5.12) | 100 |
| 2 GHz (Plane Wave) | Minimum | (PARA 4.5.12) | 100 |
| 10 GHz (Plane Wave) | Minimum | (PARA 4.5.12) | 100 |

-  2  -

Conductive Fluorosilicone Elastomer  (5000 Series) (Cont.)

| Properties (General Specifications for Silver Aluminum Fluorosilicone Elastomer) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Hardness (Shore A) | Tensile (psi) | Elongation (min. – max.) | Tear (lb./in) | Operating Temperature Deg. C (min. to max.) | Specific Gravity (g/cc) |
| 75 | 200 | 100 - 300 | 30 | -55 to +125 | 4.0 |

HUBZONE  Certified  and  Veteran  Owned  Manufacturer

MAJR   Products  Corporation

17540  State  Highway  198

Saegertown,   PA   16433

PH:  (814) 763-3211   FX:  (814) 763-2952

www.majr.com     email;  sales@majr.com